## Slide 1: 二极管交流小信号特性分析

## Slide 2: 猫须探测器 cat whisker detector
卡尔·费迪南德·布劳恩
  Karl Ferdinand Braun
▪ 发明阴极射线管
▪ 改进无线电通讯
▪ 无线电接收机
▪ 无线电发射机
  1909年度诺贝尔物理学奖
L
D
C
RL
PbS 猫须探测器
布劳恩与马可尼共获1909年度诺贝尔物理学奖
无线电接收器的简化电路
音频信号
调幅波
斩波
C:高频滤波电容
L:电感上产生射频电压
1904年弗莱明发明的真空管（整流，放大）
二战时真空管无限风光
http://makearadio.com/misc-stuff/catswhisker.php
在古董和收藏家市场上可以看到

## Slide 3: 小信号交流分析
I0
V0
vs:输入小信号
is:小信号响应

## Slide 11
交流导纳：

## Slide 13
二极管直流电导也叫做扩散电导，其倒数叫做PN结扩散电阻。
称为P-N结扩散电容。是正偏压下PN结准中性区中存贮电荷随偏压变化引起的电容，随直流偏压的增加而增加。所以，在低频正向偏压下，扩散电容特别重要。

## Slide 14: 小提示
以上讨论，前提条件是交流信号的周期远大于载流子在准中性区中扩散所需要的时间。这样在扩散区中空穴随位置的变化函数可以认为是稳态分布的 。
在正向偏置下扩散电容要远大于势垒电容。
T=300K,Nd=51016,Na= 51015,VR=5V, 势垒电容C=0.366pF.

## Slide 15
二极管小信号等效电路

## Slide 16
Au/n-SiC/Au
1.频率的关系
2.扩散电容远大于势垒电容

## Slide 17: 作业
Consider a P+N silicon diode at T=300K. The diode is forward biased at a current of 1 mA. The hole lifetime in the n region is 10-7 s. Neglecting the depletion capacitance calculate the diode impedance at frequencies of 10 kHz, 100 kHz, 1MHz and 10MHz.
Consider a P+N silicon diode at T=300K. The slope of the diffusion capacitance versus forward-bias current is 2.510-6 F/A. Determine the hole lifetime and the diffusion capacitance at a forward-bias current of 1mA.